# Light Reflectance Values of STUDIO Collection® Architectural Resin Sheets

This technical bulletin provides the Light Reflectance Values (LRV) of STUDIO Collection® Architectural Resin sheets. Light Reflectance Value measures the amount of light reflected by a material. Values were measured using the method described in ASTM C609 - Measurement of Light Reflectance Value and Small Color Differences Between Pieces of Ceramic Tile. Stain Resistance

The following reagents show no lasting effects on the surface of STUDIO Collection® Architectural resin sheets when tested to the ISFA 2-01 Cleanability/Stain Resistance standard.

### Studio Collection®

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| NUMBER | NAME | LRV |  | NUMBER | NAME | LRV |
| **8560** | Amber Glass | 12.4 |  | **8200** | Kaleidoscope | 60.1 |
| **8455** | Antique Glass | 19.4 |  | **8586** | Luna | 16.9 |
| **6720** | Bellissimo | 53.0 |  | **1050** | Midnight Sky | 4.80 |
| **7100** | Black Ice | 6.50 |  | **8601** | Neptune | 25.0 |
| **1800** | Calacatta Stone | 73.3 |  | **8320** | New Calderon | 8.70 |
| **8330** | Cat Eye | 24.1 |  | **8580** | Night Pearl | 4.80 |
| **8346** | Celestial Pearl | 27.6 |  | **8500** | Nougat | 50.1 |
| **8425** | Cement | 14.1 |  | **8700** | Ocean Breeze | 9.60 |
| **8344** | Charcoal Pearl | 14.7 |  | **8343** | Pearl | 59.3 |
| **8608** | Cirrus II | 36.2 |  | **8585** | Silver Comet | 18.5 |
| **8485** | Cobalt Glass | 5.50 |  | **8345** | Silver Pearl | 21.8 |
| **8570** | Copper Canyon | 5.30 |  | **8600** | Sirocco | 39.2 |
| **6600** | Cottonwood | 86.2 |  | **8465** | Sky Glass | 14.8 |
| **8575** | Cozumel | 79.2 |  | **8710** | Tempest | 67.4 |
| **8770** | Ebony Twist | 5.30 |  | **8587** | Terra | 23.0 |
| **8480** | Frosted Glass | 23.3 |  | **8760** | Transcendent | 70.4 |
| **8495** | Gold Mine | 7.50 |  | **8340** | Tusk | 18.6 |
| **8810** | Grenadine | 6.00 |  | **1060** | Twinkle | 75.2 |
| **8570** | Honey Crunch | 9.30 |  | **8609** | Whimsy | 37.1 |
| **8606** | Irish Bell | 25.3 |  | **6636** | White Sands | 56.6 |

|  |
| --- |
| **Note: for cautions and information on exposure to any Aristech Surfaces’ product, please see the applicable material safety data sheet.** |

**Information contained herein** is: a) based on Aristech Surfaces’ available technical data and experience; b) intended only for individuals having applicable technical skill, with such individuals assuming full responsibility for all design, fabrication, installation, and hazards; c)to be used with discretion and at one’s own risk, after consultation with local codes and with one’s independent determination that the product is suitable for the intended use; and d)not to be used to create designs, specifications, or installation guidelines. **Aristech Surfaces makes no representation, or warranty, express or implied, and assumes no liability or responsibility as to**: i) the accuracy, completeness or applicability of any supplied information; ii) results obtained from use of the information, whether or not resulting from Aristech Surfaces’ negligence; iii) title, and/or non-infringement of third party intellectual property rights; iv) the merchantability, fitness or suitability of the product for any purpose; or v) health or safety hazards resulting from exposure to or use of the product. **Aristech Surfaces shall not be liable** **for** x) any damages, including claims relating to the specification, design, fabrication, installation, or combination of this product with any other product(s), and y) special, direct, indirect, or consequential damages.