# Light Reflectance Values of STUDIO Collection® Architectural Resin Sheets

This technical bulletin provides the Light Reflectance Values (LRV) of STUDIO Collection® Architectural Resin sheets. Light Reflectance Value measures the amount of light reflected by a material. Values were measured using the method described in ASTM C609 - Measurement of Light Reflectance Value and Small Color Differences Between Pieces of Ceramic Tile.  Stain Resistance

The following reagents show no lasting effects on the surface of STUDIO Collection® Architectural resin sheets when tested to the ISFA 2-01 Cleanability/Stain Resistance standard.

### Studio Collection®

| ### NUMBER | ### NAME | ### LRV |  | ### NUMBER | ### NAME | ### LRV |
| --- | --- | --- | --- | --- | --- | --- |
| ### 8560 | Amber Glass | 12.4 |  | ### 8200 | Kaleidoscope | 60.1 |
| ### 8455 | Antique Glass | 19.4 |  | ### 8586 | Luna | 16.9 |
| ### 6720 | Bellissimo | 53.0 |  | ### 1050 | Midnight Sky | 4.80 |
| ### 7100 | Black Ice | 6.50 |  | ### 8601 | Neptune | 25.0 |
| ### 1800 | Calacatta Stone | 73.3 |  | ### 8320 | New Calderon | 8.70 |
| ### 8330 | Cat Eye | 24.1 |  | ### 8580 | Night Pearl | 4.80 |
| ### 8346 | Celestial Pearl | 27.6 |  | ### 8500 | Nougat | 50.1 |
| ### 8425 | Cement | 14.1 |  | ### 8700 | Ocean Breeze | 9.60 |
| ### 8344 | Charcoal Pearl | 14.7 |  | ### 8343 | Pearl | 59.3 |
| ### 8608 | Cirrus II | 36.2 |  | ### 8585 | Silver Comet | 18.5 |
| ### 8485 | Cobalt Glass | 5.50 |  | ### 8345 | Silver Pearl | 21.8 |
| ### 8570 | Copper Canyon | 5.30 |  | ### 8600 | Sirocco | 39.2 |
| ### 6600 | Cottonwood | 86.2 |  | ### 8465 | Sky Glass | 14.8 |
| ### 8575 | Cozumel | 79.2 |  | ### 8710 | Tempest | 67.4 |
| ### 8770 | Ebony Twist | 5.30 |  | ### 8587 | Terra | 23.0 |
| ### 8480 | Frosted Glass | 23.3 |  | ### 8760 | Transcendent | 70.4 |
| ### 8495 | Gold Mine | 7.50 |  | ### 8340 | Tusk | 18.6 |
| ### 8810 | Grenadine | 6.00 |  | ### 1060 | Twinkle | 75.2 |
| ### 8570 | Honey Crunch | 9.30 |  | ### 8609 | Whimsy | 37.1 |
| ### 8606 | Irish Bell | 25.3 |  | ### 6636 | White Sands | 56.6 |

### Note: for cautions and information on exposure to any Aristech Surfaces’ product, please see the applicable material safety data sheet.

Information contained herein is: a) based on Aristech Surfaces’ available technical data and experience; b) intended only for individuals having applicable technical skill, with such individuals assuming full responsibility for all design, fabrication, installation, and hazards; c)to be used with discretion and at one’s own risk, after consultation with local codes and with one’s independent determination that the product is suitable for the intended use; and d)not to be used to create designs, specifications, or installation guidelines.  Aristech Surfaces makes no representation, or warranty, express or implied, and assumes no liability or responsibility as to: i) the accuracy, completeness or applicability of any supplied information; ii) results obtained from use of the information, whether or not resulting from Aristech Surfaces’ negligence; iii) title, and/or non-infringement of third party intellectual property rights; iv) the merchantability, fitness or suitability of the product for any purpose; or v) health or safety hazards resulting from exposure to or use of the product.  Aristech Surfaces shall not be liable for x) any damages, including claims relating to the specification, design, fabrication, installation, or combination of this product with any other product(s), and y) special, direct, indirect, or consequential damages.