# Physical Properties

Bulletin 185
07/13/2021

Aristech Surfaces AcrySPA™ is a composite engineered material which has the exceptional surface properties, weathering characteristics and aesthetics of Aristech Surfaces Opaque Continuous Cast Acrylic and a substrate that imparts outstanding impact resistance and thermoformability.

| Property | Typical Values | Units | Test Method |
| --- | --- | --- | --- |
| General: Thickness Specific Gravity | 0.160 (4.1) 1.085 | Inch (mm) — | — ASTM D-792 |
| Mechanical: Tensile Strength Tensile Modulus Tensile Elongation Flexural Strength (Acrylic in Compression) Flexural Modulus (Acrylic in Compression) Flexural Strength (Acrylic in Tension) Flexural Modulus (Acrylic in Tension) Notched Izod Impact Falling Dart Impact Barcol Hardness Rockwell Hardness (M) | 6,600 (45.5) 370,000 (2,551) 4.4 9,100 (62.7) 340,000 (2,344) 10,800 (74.5) 326,000 (2,247) 2.1 (11.0) 12.3 (16.7) 54 67 | psi (MPa) psi (MPa) % psi (MPa) psi (MPa) psi (MPa) psi (MPa) Ft.lbs./in.of notch (kJ/m2) Ft.lbs. (J) — — | ASTM D-638 ASTM D-638 ASTM D-638 ASTM D-790 ASTM D-790 ASTM D-790 ASTM D-790 ASTM D-256(Method A) FTMS 406 M-1074 ASTM D-2583 ASTM D-785 |
| Thermal: Hot Forming Temperature (Acrylic Side) (ABS Side) Coefficient of Thermal Expansion DTUL @ 264 psi(1.82 MPa) | 350-380 (177-193) 300-340 (149-171) 0.000047 (.000085) 186.0 (85.6) | ˚F (˚C) ˚F (˚C) in./in./ ˚F (cm/cm/˚C) ˚F (˚C) | Aristech Method Aristech Method ASTM D-696 ASTM D-648 |
| Miscellaneous: Water Absorption Gardner Gloss (60 Angle) Odor Taste | 0.19 87.4 None None | % — — — | ASTM D-570 ASTM D-523 — — |

Note: for cautions and information on exposure to any Aristech Surfaces’ product, please see the applicable material safety data sheet.

Information contained herein is: a) based on Aristech Surfaces’available technical data and experience; b) intended only for individuals having applicable technical skill, with such individuals assuming full responsibility for all design, fabrication, installation, and hazards; c)to be used with discretion and at one’s own risk, after consultation with local codes and with one’s independent determination that the product is suitable for the intended use; and d)not to be used to create designs, specifications, or installation guidelines.  Aristech Surfaces makes no representation, or warranty, express or implied, and assumes no liability or responsibility as to: i) the accuracy, completeness or applicability of any supplied information; ii) results obtained from use of the information, whether or not resulting from Aristech Surfaces’ negligence; iii) title, and/or
non-infringement of third party intellectual property rights; iv) the merchantability, fitness or suitability of the product for any purpose; or v) health or safety hazards resulting from exposure to or use of the product.  Aristech Surfaces shall not be liable for x) any damages, including claims relating to the specification, design, fabrication, installation, or combination of this product with any other product(s), and y) special, direct, indirect or consequential damages.