# **General Properties: Grades GPA, 1-300 & S-300**

Bulletin 130  
07/15/2021

Aristech Surfaces Acrylic Sheet products are continuous cast and derived from unique formulations. Aristech Surfaces Acrylic Sheet GPA is a general purpose acrylic sheet. It is solvent cementable, and it can be ordered in many standard col-ors, thicknesses, and sizes. GPA is ideally suited for signs, fabricated products and general distribution. Aristech Surfaces Acrylic Sheet I-300/S-300 is a cross-linked solvent resistant acrylic sheet with exceptional thermoforming characteristics making it ideally suited for applications such as sanitaryware. Aristech Surfaces Acrylic Sheet I-300/S-300 is available in standard colors and is produced to customers’ orders in many thicknesses and sizes.Novitates autem si spem adferunt

## Unlimited Length

Because Aristech Surfaces Acrylic Sheet is con tinuously cast, it can be produced in either reels or sheets of lengths limited only by the practicality of shipping and handling weights and sizes. This elimi nates unsightly and costly seams and joints in finished products.

## Reel Concept

Aristech Surfaces Acrylic Sheet is available in reels, providing additional savings, a variety of efficient handling and fabricating techniques, and allowing re duced invento-ries-permitting the use of storage space for production.

## Closer Thickness Tolerance

A thickness tolerance of ± 10% or ± .015” (0.4 mm), which-ever is greater, is maintained in Aristech Surfaces Acrylic Sheet, assuring uniformity. This uniformity reduces the rate of rejections attributable to breakage, thinning out or vari-ances in light transmission.

## Availability

Aristech Surfaces Acrylic Sheet can be supplied in widths from 24” to 108” (60 to 275 cm). Sheet thicknesses range from 0.080” to 0.236” (2 to 6 mm). Aristech Surfaces Acrylic Sheet can be cut to fraijctional sizes to comply with close tolerances required by MilSpecs or customer specifications.

## Design Freedom

With larger sizes, better uniformity and superior proper ties, Aristech Surfaces Acrylic Sheet opens new horizons for product designs never possible with con ventional cell-cast acrylic sheet. Aristech Surfaces Acrylic Sheet gives design-ers freedom in colors, too. Aristech Surfaces Acrylic Sheet is supplied in a variety of standard and marbleized colors and, by request, the Aristech Surfaces color laboratory can develop other colors that may be required.

## Formability

Aristech Surfaces Acrylic Sheet can be cold formed at room temperatures to yield generous curved surfaces. If unusual shapes or smaller curvatures than those possible with cold forming are desired, Aristech Surfaces Acrylic Sheet can be thermoformed. This involves heating the material to approx-imately 380° F (195° C), and forming the desired shape with vacuum or air pressure.

## Fabrication

Unlike glass and other materials, Aristech Surfaces Acrylic Sheet can easily be sawed, drilled, routed, filed, cemented, and machined. It behaves similar to hard wood or brass.

## Resistance To Breakage

Aristech Surfaces Acrylic Sheet has 10 to 17 times great-er breakage (impact) resistance than glass in equivalent thicknesses. Unlike other plastics used in glazing, Aristech Surfaces Acrylic Sheet does not lose its outstanding break-age resistance because of degradation from weathering.

## Light Weight

Aristech Surfaces Acrylic Sheet is about 46% as heavy as ordinary glass.

## Safety

The resistance to breakage and lighter weight of Aristech Surfaces Acrylic Sheet make it a safer material to handle and work with. If breakage should occur, the material does not shatter and splinter. Usually the break is local (a hole) or a clean single break. The broken edges are dull com-pared to glass fragments. Several state and local building code agencies specify acrylics over ordinary glass for storm door and other glazing applications where safety is the main criterion.

## Weather Resistance

Aristech Surfaces Acrylic Sheet has outstanding weather-ing resistance. Even in areas such as Florida and Arizona, acrylics are virtually unaffected after 15 or more years exposure. Acrylics have been used suc cessfully in aircraft glazing since before World War I I and for more than 40 years in outdoor sign applications.

## Optical Clarity

Light transmittance for clear Aristech Surfaces Acrylic Sheet is about 93% compared to 88% for ordinary glass.

## Resistance To Temperature Extremes

The continuous use temperature for Aristech Surfaces Acrylic Sheet is up to 180° F (82° C). Higher temperatures can be tolerated for short periodsoftimewithout permanent damage occurring. At extremely low temperatures (-30° F) (-34.4 ° C), Aristech Surfaces Acrylic Sheet remains very serviceable with only a slight reduction in breakage resis-tance occurring.

## Insulating Values

Aristech Surfaces Acrylic Sheet is a better insulator than glass. Its heat transfer characteristics 1ire similar to those of rubber. The coefficient of thermal conductivity (K Fac-tor) or ability to conduct heat is 1.4 compared to 5 to 6 for ordinary glass. This means with zero wind velocity on both sides of the window pane, ordinary glass conducts heat more than 4 times as fast as Aristech Surfaces Acrylic Sheet. The overall coefficient of heat transmission (U Fac-tor) is 1.04 compared to 1.25 for glass. At these conditions, Aristech Surfaces Acrylic Sheet is still approxi mately 20% better insulator than ordinary glass.

## Standards

Aristech Surfaces Acrylic Sheet will meet and/or exceed the following specifications:

* ASTM D 4802-02 Category A-2, Finish 1 and 2, Type UVF. Exception: Thickness tolerance shall be as listed on front page of this bulletin.
* American National Standards Institute Specifications:  
  • ANSI-Z-124.1-Plastic bathtub units.  
  • ANSI-Z-124.2-Plastic shower units.  
  • ANSI-Z-124.3-Plastic lavatories
* International Association of Plumbing & Mechanical Officials (IAPMO)
* Material and Property Standards for Acrylic-Faced Bathtubs, Tub-showers and Lavatories.
* Material and Property Standard for Acrylic-Faced Spas

|  |
| --- |
| **Note: for cautions and information on exposure to any Aristech Surfaces’ product, please see the applicable material safety data sheet.** |

**Information contained herein** is: a) based on Aristech Surfaces’available technical data and experience; b) intended only for individuals having applicable technical skill, with such individuals assuming full responsibility for all design, fabrication, installation, and hazards; c)to be used with discretion and at one’s own risk, after consultation with local codes and with one’s independent determination that the product is suitable for the intended use; and d)not to be used to create designs, specifications, or installation guidelines. **Aristech Surfaces makes no representation, or warranty, express or implied, and assumes no liability or responsibility as to**: i) the accuracy, completeness or applicability of any supplied information; ii) results obtained from use of the information, whether or not resulting from Aristech Surfaces’ negligence; iii) title, and/or non-infringement of third party intellectual property rights; iv) the merchantability, fitness or suitability of the product for any purpose; or v) health or safety hazards resulting from exposure to or use of the product. **Aristech Surfaces shall not be liable** **for** x) any damages, including claims relating to the specification, design, fabrication, installation, or combination of this product with any other product(s), and y) special, direct, indirect or consequential damage.